## Dislocation Theory and Dislocation Simulation
How is plastic deformation defined?
Deformation that remains when load is removed

What is preserved during deformation?
Lattice structures

What does the preservation of the lattice structure imply?
- That the atoms are sheared against each other
  - the deformation is ‚quantized‘ in terms of multiple lattice vectors

When does atomistic slip occur?
- at low temperatures
- at high stresses

Through which parameters is a slip system characterized?
- Slip plane normal s
- slip direction n
- slip vector (a lattice vector in slip direction)

Which planes are the slip planes?
The densest packed ones

Which directions are the slipe directions?
The densest packed ones

How is the plastic distortion tensor defined?
bold %beta_p = sum from %alpha %gamma^%alpha bold B^%alpha
B: Unterlagen

How is plastic strain tensor defined?
bold %varepsilon _ p = bold %beta_p^(s) = sum from %alpha %gamma^%alpha bold M^%alpha
Mα: projection tensor

How many slip systems are needed at least to build up a plastic deformation state?
5
Why 5?
Unterlagen

What is driving force for shear on a slip system?
Resolved shear stress

What is the work conjugate of the resolved sheat stress?
Resolved shear strain

How can the resolved shear stress be derived from the stress tensor?
By (double) contraction with the projection tensor Mα: %tau^%alpha = bold M^%alpha : bold %sigma

In which direction is the shear stress maximum in a tensile test?
The direction pointing in 45° angle to the loading directions

How do lattice planes slip?
Atom by atom

By which parameters is a dislocation defined?
- Slip vector (Burgers vector): b
- slip plane
- tangent vector (parallel to the line direction) : t

How is the Burgers vector defined?
The vector that is missing for making a closed path around the dislocation

How are Burgers vector and dislocation line oriented to each other in an edge dislocation?
Perpendicular

How are Burgers vector and dislocation line oriented to each other in a screw dislocation?
Parallel

How can one visualize the three ways of creating a straight dislocation line?
Volterra construction

What is a good definition of a dislocation?
A dislocation is a boundary of a slipped area

Through which forces do the dislocations move?
Peach-Koehler forces:
bold F_PK = ( bold %sigma cdot bold b) times bold t

How is the Peach-Koehler force oriented to the dislocation line?
Normal to it (perpendicular)

Does the full Peach-Koehler force move the dislocation?
No, only the glide component Fg parallel to the glide plane is responsible for the glide

How is the velocity of the dislocation oriented to the dislocation?
Normal to it (perpendicular)

Which velocity is higher? Glide or Climb?
Glide by far
Why?
Because climb needs additionally removal or addition of material

How is the dynamics of dislocations?
Aristotelian – overdamped

What are different types of velocity laws for dislocations?
- Linear
- Exponential
- Power law

How is the linear velocity law for dislocations defined and which physical phenomena play a role?
- It is caused by phonon drag on the dislocation
- dislocations scatter sound waves --> friction force
- The friction controls and minimizes too high velocities

How is the exponential velocity law for dislocations defined and which physical phenomena play a role?
Thermal activation obstacles and Peierls barriers

What is the Peierls barrier / Peierls stress?
Stress to break the atomic bonds (while moving the dislocation)

How is the power law velocity for dislocations defined and which physical phenomena play a role?
v = left( %tau over %tau_0 right)^n
- Pure phenomenologic
- no physics

By which internal stresses is the stress that moves the dislocations opposed?
- Peierls stress
- stress required to cross obstacles
- stress induced by other dislocations (e.g. work hardening)

How do you construct a dislocation loop?
- Choose a surface inside the material with closed boundary dS
- displace boundaries by b
- relax the material

For an arbitrary shear strain field it is possible to construct a corresponding dislocation density field (the dislocations are the contour lines of the shear strain field).

What are geometrical necessary dislocations?
Dislocations associated with a heterogeneous plastic strain state (on a given scale of resolution)

How is the relation between the stress field of dislocations, their strain field and the stress field of the material?
If we can evaluate the stress field of dislocations, then we also can evaluate the (global) stress field associated with the shear strain field of the dislocations

Which kind of problems can be solved with the stress field of screw dislocations?
Anti-plane strain problems

Which kind of problems can be solved with the stress field of edge dislocation?
Plane strain problems

What are anti-plane strain problems?

What is a single-valued displacement field (for a deformed body)?

What is compatibility condiition for a strain / distortion field?
lint from S bold %beta {} d bold s = 0
β: distortion

Does the compatibility condition need to be fulfilled for both elastic and plastic distortion?
No, only in sum (elastic + plastic) it needs to be fulfilled

Where is the incompatibility of the elastic field placed looking at a dislocation?
In the dislocation line (elastic singularity)

Can dislocations be formed in thermal equilibrium?
No, the formation energy is much to high (above 1eV per b)

How does one solve the stress problem of a screw dislocation near a boundary?
- Condition: Surface must be traction-free
- place an image screw dislocation of opposite sign on the other side
  - the dislocation experiences an attractive force towards the boundary because of image interaction

Which problem does an infinte straight screw dislocation describe?
Anti-plane strain problem

Which components of the displacement vector and the strain tensor do not vanish?
- non-vanishing displacements: uz
- non-vanishing strain components: εxz und εyz

Which problem does an infinte straight edge dislocation describe?
Plane strain problem

Which components of the displacement vector, the strain and the stress tensor do not vanish?
- non-vanishing displacements: ux und uy
- non-vanishing strain components: εxx, εxy und εyy
- non-vanishing stress components: σxx, σxy, σyy und σzz

With which kind of functions is the general plane strain problem solved?
Airy stress function

What are the pre-requisites for solving the stress problem of an infinite straight edge dislocation?
- A spatial decay with 1/r (why? --> Unterlagen)
- Solution must be zero an x-axis (why? --> Unterlagen)
- Solution must have a maximum at the positive y-axis and a minimum at the negative y-axis (why? --> Unterlagen)

What is the formula for the elastic energy of an infinite straight edge dislocation?

E = { Gb^2 } over { 4 %pi } ln left ( R_0 over r_i right )
- R0: outer radius (grain size)
- ri: inner cut-off radius

How is the problem with an edge dislocation sitting close to a boundary solved?
- The stress on the boundary must be zero (why actually?)
- put an image dislocation of opposite sign onto the other side
  - does not fully remove the shear stress --> put dislocations with Burgers vector in y-direction onto the surface

How do pile-ups form?
For example through dislocation sources like a Frank-Read source

How does the stress field from the obstacle in direction of the dislocations look like?
Like 1/r	(image)

Where does the formation of pile-ups leads to?
The Hall-Petch law for polycrystalline hardening (The material is harder when the crystalls are smaller)

What can be envisaged as a planar array of edge dislocations?
(Tilt) Grain Boundary

Is the same true for a twist boundary and screw dislocations?
- No, a twist boundary cannot easily be formed through a planar array of screw dislocations
- a network of screw dislocation is necessary

How is the self-interaction of a dislocation described?
- For fairly short segments, where the dislocation can be envisaged as almost straight, the dislocation can be treated as rubber string
  - the line tension does not depend on the overall configuration of the dislocation and is basically constant

Which forces play a role at the interaction between dislocations and obstacles?
- Dislocation self-interaction (line tension)
- interaction with obstacles
- external forces (induced by external stresses)

Which kinds of obstacles do exist?
- Strong obstacles
- Weak obstacles

What are strong obstacles?
- Even a single obstacle leads to strong deformation of dislocation (precipitates, ...)
- but they might be easier to pass than the weak obstacles

What are weak obstacles?
- Only the cumulative action of many obstacles leads to deformation of the dislocation (vacancies, solute atoms, ...)
- but because they are so many they might be harder to pass than the strong obstacles

What happens at infinitely strong obstacles?
The dislocation passes by leaving a loop

What happens at very weak obstacles?
The dislocation remains almost straight, and is actually pinned at the obstacles

What is a discrete dislocation simulation?
Looking at the motion of dislocations under the influence of external stresses and interaction with other defects

How is the atomic arrangement put into the dislocation simulation?
By properties attached to the dislocation lines

Which parameters can be altered in dislocation simulation?
- Core radius
- line tension model
- mobility parameter
- annihilation distance
- etc.

What can dislocation simulations be used for?
- Validation of continuum models
- dteermination of microscale stress strain curves
- understanding microscale mechanisms by switching certain mechanisms on/off
- analysis of strain hardening mechanisms
- (understanding size effects)

What are the limits of dislocation simulations?
- Short length scales
- high strain rates (typically ~10² s-1)
- difficulties with interactions at the boundary
- small details (i.e. changes in parameters) may change a lot
- complex sample geometries are hard to simulate
- still the most simulations are carried out for the easiest case of isotropic elasticity

What are the main problems of dislocation simulations?
- Long-range nature of dislocation stresses (everything interacts with everything)
- intermittent (pulsierend) dynamics: most of the time nothing happens and then at some point rapid avalanches occur

What are the assumptions for 2D dislocation simulations?
- Rigid, straight, parallel dislocations, which cat like point particles in 2D
- either edge or screw dislocations (WHY?)

What are the disadvantages of 2D dislocation simulations?
- 3D effects cannot be represented
  - can be met by including certain rules to mimic 3D behaviour

How are boundary conditions imposed at dislocation simulations (no periodic BCs)?
- Summation of
  - stress field of dislocations in infinte body
  - stress field in dislocation free body with modified surface displacements/tractions

How are periodic BCs applied to dislocation simulations?
Problem: long range stress fields (summation over infinitely many image stresses necessary), this is why:
- At first analytical calculation of stress field perpendicular to burgers vector direction
- then numerical calculation of stress field in burgers vector direction (over finite amount of dislocation walls)
- error for stress field is quite small

     The method above is only for dislocations possible which are aligned parallel to the simulation box boundaries. What does one do for not perfectly aligned dislocations?
Split their Burgers vectors in partial Burgers vectors which are aligned to the boundaries

What is the problem wih climb in dislocation simulations?
It is much slower than glide (therefore, often only glide motion is considered)

What kind of different dynamics are possible in a dislocation dynamics simulation?
- Continuous (MD-like)
- discontinuous (Monte Carlo – like)

What is a possible Monte-Carlo moving criterion for dislocations?
- Only the dislocation with the highest stress is moved
- (fair representation of temperature activated movement of dislocations)

Why discontinuous simulation methods for dislocation simulations so fast?
Because the interactions are tabulated and do not need to be calculated

Which motion is considered in continuous dislocation simulations?
Aristotelian

How are the possibilities to represented dislocation lines in a 3D dislocation simulation?
- As a sequence of straight segments with discrete orientations
- as a sequence of straight segments with arbitrary orientations
- as parametric splines

How is the scheme for moving dislocation lines?
- Evaluate forces
- Evaluate velocities
- move segments
- Adjust segment lengths and/or remove segments

What are problems concerning the discrete representation of dislocations?
- Choice of fixed orientations has big influence on some mechanisms
- interaction between dislocations is badly represented

How does the continuous scheme look like for dislocation movement?
1. Calculation of nodal forces
2. Calculation of nodal velocities
3. numerical time integration
4. topological changes

Which kinds of dislocation reactions do exist?
Junction formations
- Lomer reaction
- glissile reaction
- Hirth reaction
- collinear reaction
How do they look like?

- Cross slip of screw dislocations
- dislocation annihilation
- absorption, transmission, etc. at interfaces/surfaces

How is the relation between FEM and DDD in a simulation?
- The FEM provides results for the stress field in volume (which is used for determining interactions in the DDD simulation
- The DDD part sends information about the dislocation microstructure to the FEM (where it is used as input for the calculation of boundary conditions for the micro components)

How are the initial conditions set for a discrete dislocation simulation (different possibilities)?
- Random segments with pinned endpoints (unphysical since dislocations cannot inside the crystal)
- introduce random straight lines from surface to surface and relax
- introduce random loops and relax
- cutting out simulation box from prestrained larger volume

Which possibilites exist to simplify the simulations of dislocations?
Make generalized continuum models

What are the advantages of generalized continuum models?
- One value can represent many discrete elements
  - reduce computational costs

The equations for dislocations (movement, stresses, etc.) are invariant. What does that mean?

What does the DFT formulation for dislocations aim?
By reformulating the dislocation dynamics in a continuum setting one might be better able to see how (or not) engineering plasticity represents the microscale processes at its physical origin