Multiscale Simulation Methods – Summary

Introduction

Why do we need Simulations?
- Behaviour of materials is too complicated
- Normal methods like tensile tests only provide us with simple results
- Many effects on different time and length scales
- Some experiments are just too expensive or not even executable
- Simulations are repeatable up to 1 million times

Why do we need Multiscale Simulation Methods?
Only reason in my opinion: Because we cannot use Molecular Dynamics on large length scales

Which definitions of Multiscale Modelling are possible?
- 2 definitions:
  - different simulation techniques on different time and length scales (pick always the one which fits best to the current problem)
  - connect different simulation methods into one big simulation

How can the length scale spanning simulations be divided into two groups?
- Concurrent Modelling
- Sequential Modelling

Describe Concurrent Modelling (gleichzeitig)
- in the region of interest increase the number of degrees of freedom
- in this way a much higher resolution is gained at this area
- Problems:
  - How are the boundaries treated?
  - How shall the different time scales be treated?

Describe Sequential Modelling (fortlaufend)
- Layers of different homogenization are layed out onto the simulation body
- Then the information from the finest layer are transferred to the next coarser layer and so on
- Problem:
  - Information can be lost during the transformation (through homogenization)

# Homogenization Aspects and Effective Material Properties

General
- Examples:
  - heterogeneous systems with different scales
  - solid matrix with voids (filled with a fluid)
  - nature: rocks, sand, beds, sponges, woods, soil
- which information do we want to get?
  - (effective) Diffusion
  - ( ---- ) Dispersion
  - ( ---- ) Permeability
  - ( ---- ) mechanical Properties
  - no detailed properties / description of the material

What are homogenization methods good for?
- Reducing the dimensions of the simulation
- Or finding a homogeneous counterpart to the heterogeneous material

What are the steps of a homogenization simulation?
1. Identify type of inhomogenity (pores, inclusions, ...) + model the inhomogeneous medium
2. Derive the effective material properties (= homogenization)
3. Simulate on macroscale (with homogeneous properties)

In the first step the microscopic simulation is changed into a macroscopic	description; what are the advantages and disadvantages of a macroscopic	description?
- Disadvantage: A totally new description for each material point needs to be developed
- Advantage: No interactions at the interface between two different regions need to be considered

Which homogenization techniques are possible?
1. Volume fractions
2. Representative Volume Elements (RVE)

How is the mathematical description for including volume fractions?
Axel fragen, ob das für die Klausur wichtig ist

How are RVEs defined?

How is the simulation on the macroscale carried out?
Like a normal continuum simulation (displacement functions, deformation gradient, ...)

Example: Diffusion

How is the effective diffusivity defined?
The eff. diffusivity describes the diffusion through the pore space and is macroscopic in nature

D_e = {D %varepsilon_t %delta } over { %tau }
D: free Diffusion
εt : Transport Available Porosity
δ : constrictivity
τ : tortuosity

What is free diffusion?
The diffusion of the diffusing species in the pore medium (fluid)

What is Transport Available Porosity?
fraction of pore volume available for the diffusion (= all pores minus pores which are not accessible for the diffusing particles (e.g. because their are not connected to the rest of the pore system, they are to small for the diffusing particles))

What is constrictivity?
C. describes the slowing down of diffusion due to the higher viscosity in narrow pores as a result of the greater proximity to the pore walls

What is tortuosity?
T. is the fraction between the euclidian distance of two points (e.g. at the two ends of the simulated system) and the actual shortest path through the network

# Molecular Dynamics
What is the definition of MD?
A simulation tool where the temporal evolution of every atom in a specimen is explicitly described

What is the different between MD and Monte Carlo simulations?
- Monte Carlo simulations are good in describing equilibrium situations
- The temperature in Monte Carlo simulations is controllable
        - Simulation of phase transitions
- But it does not provide any information about dynamics
        - NO calculation of diffusion coefficients possible

How many atoms can be simulated in an MD simulation?
About 1 million

Which equations does the movement of the atoms follow?
Newton‘s equations of motion	(F = ma)

Which approximations are made in MD?
- Born-Oppenheimer approximation
  - my definition: Electrons move instantaniously with the nuclei
  - definition of slides: Nuclei are so heavy that their velocity is much smaller than the velocity of the electrons. This is why the wave functions of nucleus and the electrons can be seperated:
    %PSI _molecule = %PSI_electrons times %PSI_nuclei
- The mass of the atoms is concentrated as point in the atom core
  - So the atoms can be envisaged as classical particles and we can use classical mechanics

What are the initial information needed for an MD simulation?
- Initial positions and velocities
- BCs
- interaction potential(s)

Which types of boundary conditions do exist?
- free BC
  - all surface atoms can move into arbitrary directions
- force BC
  - prescribe extra forces to the surface atoms
- fixed BC
  - some DOF are constrained for the surface atoms
- periodic BC
  - atoms at the surface interact with those from the opposite side
  - the system is essentially surface-free
- mixed BC
  - combination of e.g. fixed BC in x-direction and force BC in y-direction

What are the properties of periodic BCs?
- Allows to reduce highly the number of particles
- particles at the surface experience similar forces to particles in the bulk material
- forces at a particle in the central box are dependent on particles in every neighbouring box

How is the cut-off at periodic BCs defined?
The particle does not interact with its counterpart in a neighbouring box

Why must one not apply periodic BCs at single dislocations?
- The stress field of a single dislocation (with line direction in z) is not symmetric in the x-y-plane
- But: periodic BCs are possible with dislocation dipoles (symmetric stress field in x-y-plane)

How many neighbouring boxes does a simulations box with periodic BCs have?
- 2D: 8
- 3D: 26

How are the initial velocities set up?
- For example constant velocities for atoms at the boundary (indentation, impact)
- a certain temperature can be assigned to the system by giving its atoms a gaussian (Maxwell-Boltzmann ?) velocity distribution corresponding to 2*Tdesired and equilibrating under NVE conditions
  langle E_k rangle = {1} over {2} langle sum from{i=1} to{3N} m_i v_i^2 rangle = 3N ( k_B T ) /2
  2*Tdesired because the energy splits itself up into one half kinetic and one half potential energy

Why are interatomic potentials so important?
- These are the rules for the atomic interactions
- To calculate the forces via
  F_i = - nabla_(r(i)) U ( r_1, ..., r_N) )

What does a potential function describe?
How the energy of an N-particle system depends on the coordinates of particles 1 to N

Which parameters can effect the potential?
- Easiest case: only distance
- more sophisticated:
  - relative orientation of particles to each other
  - internal states of particles (e.g. orientation of electronic spin)
  - particle shape (?)

Which kinds of potentials do exist?
- Empirical potentials
- Semi-empirical potentials
- potentials derived only with QM (ab initio methods)
What are empirical potential functions?
Assume a functional form and fit the parameters of the function to experimental data

What are examples for empirical potential functions?
- Lennard-Jones
- Morse
- Born-Mayer

What are semi-empirical potentials?
- At first the wave function for the fixed (initial) system is calculated with QM
- some simplifications are made and experimental data replaces some parameters

What are examples for semi-empirical potentials?
- Embedded Atom Method
- Glue Model (by Ercolessi et al.)
- bond order potentials (by Tersoff and Brenner)

Which kinds of methods exist except for (semi-)empirical potential methods?
- Ab initio simulations
  - the electronic forces are directly (and only) calculated by QM
  - e.g. Car-Parinello method

How would you choose an atomic potential? What does the choice affect?
- Type of bond model (metallic, covalent, etc.)
- desired accuracy
- the requirement of universality:
  - how well does the model describe different kinds of bonds in the system?
- System size and system time
- computer resources

What is the simplest ansatz for potentials and which variations do exist?
- Pair potentials
  - hard core
  - semi-harmonic
  - soft core
- ionic interaction can be modelled pair-wise
- purely repelling interactions

How does the Lennard-Jones-potential look like?
V^LJ ( r) = 4 %varepsilon left ( ({%sigma} over {r})^12 - ({%sigma} over {r})^6 right )
- r : distance between particles (usually with cut-off)
- σ : defines a length scale
- ε : parameter for strength of interactions

Explain the course of the L-J-potential:
- repelling forces at very close distance (overlap of wave functions)
- attracting forces at far distances
- inbetween a equilibrium distance
Where do the attractive forces come from?
- For example: dipole interactions (hydrogen bonds, Van-der-Waals bonds)
- this goes with the 6th power of r reversed
  V_a ( r) = - left ({ A } over { r^6 } right )

What about the parameters ε and σ in the Lennard-Jones-Potential?
- ε is the energy at the equilibrium position
- σ is the position of the equilibrium (=distance)
- so, ε defines the energy unit, and σ defines the length unit

How can you calculate the force acting on a particle form the potential it feels?
F( r) = - ( {partial V} over {partial r} )

How can one define a temperature unit with ε?
The unit of temperature is ε/kb

How is the potential defined after the cut-off and why do we need a cut-off?
- The potential is zero ( U(r>rc) = 0 )
- It reduces the computational costs
How can one increase the computational stability of the simulation with potentials?
Scale the units into a dimensionless system

How is dimensionless scaling done?
- Set the energy, the mass and the size units to 1 (without unit)
- derive from this units all other units
  - e.g. energy
    E_new = E / %varepsilon
  - or force
    F_new = F %sigma / %varepsilon
Which side effects does dimensionless scaling have?
- The parameters σ and ε are set to unity so that they cannot be fitted anymore to materials
- all different L-J-potentials collapse into one dimensionless potential curve
  V( r ) = 4 left ( 1 over {tilde r} ^12 - 1 over {tilde r}^6 right )

What is the main step in an MD simulation?
The time integration of F = ma

Which time integration schemes do exist?
- Explicit Forward Euler
- Implicit Euler
- Runge-Kutta-Methods
- Verlet-Algorithm
  - „Leapfrog“-Algorithm / Velocity-Verlet-Algorithm

How do explicit and implicit Euler integration work?

What are the advantages of the explicit Euler scheme?
- Less information of the system is needed
- faster
- (it just takes the slope of the foregoing step)

What are the advantages of implicit Euler integration?
- Higher accuracy
- (takes time points before and after the desired time point into account)
- higher stability at longer time steps

Why does explicit Euler time integration not work for MD?
Because the scheme is not reversible, and therefore not stable (?)

What needs to be considered by setting the time step for MD?
- It must not be too big, otherwise the thermal movement of the atoms is not resolved
- smaller time steps for:
  - lighter atoms
  - higher temperatures
  - stiffer bondings
- in crystalls the time step should be around 1/10 to 1/100 smaller than the characteristic vibration frequency

What needs to be done at the postprocessing step of the MD simulation?
- Calculating strain and stress (which is really hard)
- structural analysis (defects, etc.)
# Finite Volume Method
What is the FVE?
A numerical method for solving partial differnential equaitons (PDE)

Of which terms does the PDE for field quantity consist?
- Transient term
- convection term
- diffusion term
- source (sink) term

How do the different terms look like?
- Transient
  {partial (%rho %phi)} over { partial t}
- convection
  - nabla cdot ( vec u %phi )
- diffusion
  left ( nabla cdot ( %GAMMA nabla ) right )^m %phi
- source (sink)
  S
- u, ρ, Γ and m are coefficients that must be put in by the user
- φ is the variable we want to solve for

How does the spacial discretization scheme of the FVM look like?
- Integration points are in the middle of the domains and at the face centers
- furthermore, two reference systems are set up
  - global reference system
  - local reference system

Why does one need two reference systems?
- The local one for the discretization of the equation
- the global one for repeating the discretization on all the nodes and assemble them in a global form

How are the different terms discretized?
- Transient:	- finite difference scheme
- convection:	- divergence theorem; and change integral to finite sum
- diffusion:	-	---	---	---	---	---	---
- source / sink:	- from infinte integral to finite sum

How are the values at the face center points approximated?
- Through a finite difference scheme (the average of the two neighbouring volume centers)
- usually the weighting of each of the both volume centers goes half to half but one can also change the ratio of the weighting, i.e. weight one of the volume centers more than the other one

How does the global assembly in the FVM look like?
- Basically like in the FEM/FDM: assembly of discretized equations
- Aφ = b
  - A: adjacency matrix
  - φ: variable to solve for
  - b: boundary conditions

# Amorphous Plasticity
### Shear Bands and Shear Transformations
For which kind of materials simulations of amorphous plasticity can be applied?
- Glasses
- Bulk metallic glasses

What are bulk metallic glasses?
Glasses made out of metallic elements only

What is special about glass?
- Disordered structure
- dislocations do not exist
- crystal plasticity is not applicable

How does plastic deformations in bulk metallic glasses (BMG) look like?
It deforms through building shear bands (= strain patterns with 45° orientation w.r.t. the applied shear stress)

How are individual plastic events called?
Shear transformations (ST)
What are properties of shear transformations?
- Local rearrangement of atoms
- triggered by shear stress
- not well defined volume nor shape
- their elastic interaction leads to formation of shear bands

How can an shear transformation be represented in a material?
Through an inclusion, which is undergoing a shear deformation

How can one find the stress field of such an inclusion?
- By solving the equations of elasticity
- elastic equation + infinitesimally small deformations --> Green‘s function nabla cdot %sigma + vec f = 0	+	vec f = %delta ( vec r)	--> G ( vec r, %theta ) = %sigma ( vec r, %theta ) sim {cos ( 4 %theta )} over { r^2 }
- the stress associated with an plastic event in a BMG can be represented with that function

What are the assumptions for using Green‘s functions as a solution for the stress of an ST?
- Isotropic homogeneous material
- Infinte system size
- Only shear stress
What are the problems with Green‘s functions as solutions for the stress field of inclusions?
- It requires an infinite system size
  - one cannot simulate infinte system sizes
  - so one is forced to use periodic BCs
- it leads to singularities at the position of the inclusion
  - replace the inclusion with the smallest possible dislocation loop (i.e. 4 dislocations, each rotated by 90°)
  - the stress field is exactly the same far away from it

### Model of Plasticity
In which variables is the material discretized in an amorphous plasticity simulation?
- Shear stress
- plastic strain
- energy barrier

How is the discretized energy barrier set up in an amorphous plasticity simulation?
Random to each site to represent amorphous structure

How are the plastic strain and the shear stress discretized in an amorphous plasticity simulation?
- At a point where a shear transformation happens, a unit is added to the plastic strain matrix
- then, the shear stress is updated with the stress of the shear transformation

How is chosen when and where a plastic event (= shear transformation) happens?
By the Kinetic Monte Carlo (KMC) Method

Why do we use the KMC Method?
- States are defined in terms of energy
        --> no details about the atoms are needed!
- Remark: we only choose randomly where the event happens. Other things like amount of plastic deformation of the event are constant for us

How are the steps of the Kinetic Monte Carlo Method?
1. Calculate the rates for all possible events
2. Identify simulation units and truly independent parameters
3. Calculate the probability of each event using the rates
4. Choose an event using the probabilities
5. Calculate the time that has passed since the previous event till the chosen one

How is strain softening added to the simulation?
Somehow add an exponential term which has the plastic strain as argument to the energy barrier
# Discrete Element Method
What is the Discrete Element Method?
Class of discontiniuos modelling techniques, where the material is an assembly of interacting separate particles

What are the basic ideas of the Discrete Element Method?
- Calculate all the forces acting on a particle at each time step
- obtain through the equation of motion position, velocity and acceleration of the elements at the next time step

To which fields can the DEM be applied?
- Powder metallurgy (ball mills)
- Agriculture
- pharmaceutical applications
- geotechnical studies (soil and earth crust as cohesive granular matter)
- chemical engineering
Why is DEM in these cases better than the application of continuum models?
Discontinious nature of granular materials

What are the steps in a DEM simulation?
1. Initialize the elements
2. make the neighbourhood list	<-------------------------------|
3. calculate the contact forces	|
4. solve the equation of motion for all the particles	|
5. update the particles position	|
6. go back to point 2)	-------------------------------------------------|

Which properties need to be defined for the initialization of the elements in a DEM simulation?
- Dimensions
- Shape
- Size
- Elastic Properties
- Friction, etc.

Which kind of particles are preffered for the DEM simulation and why?
Spherical particles, since the contact detection and force calculation goes much faster

What is the disadvanatge of using spheres in a DEM simulation?
They are often only an approximation

What are possible ways to generate particles for a DEM simulation?
- Delauney triangulation
- Voronoi tesselation
How does the Voronoi tesselation work?

How does the Delauney triangulation work?

How is the neighbourhood search in a DEM simulation being optimized?
At first a rough and then a fine search

What are the two approaches concerning the hardness of particles in a DEM simulation?
- Undeformable hard particles
- Undeformable elements with overlapping

For which degrees of freedom are Newton‘s equations of motion being solved?
- Translational DOF
- rotational DOF

How many differental equations need to be solved for per particle in a DEM simulation?
- 6 equations
  - so 6N equations for the whole system (N = number of particles)

Which model is employed to simulate the contact reaction between two particles?
Damped linear spring model
How can this model be extended to model friction between the particles?
Introduce a sliding friction element

For which kind of particles friction becomes more important?
For small particles

Which kind of forces can also occur between small particles?
- Adhesion forces
  - neck formation possible

Which kinds of friction do exist?
- Gliding friction
- rolling friction

How can you model a rough surface?
With half-spheres on spheres

Which forces need to be taken into account for particle-medium-interactions?
- Drag force
- Archimedes force
- Added mass force
- Magnus force
How big must be the time step in a DEM simulation?
Much smaller than the collision time (--> quite expensive computing)
Which are the possible time integration schemes for a DEM simulation?
- Euler integrator
- Verlet integrator
- Gear‘s predictor-corrector scheme

What are the advantages of the Verlet-Algorithm?
- Time reversebility
- stability

Why is the Velocity Verlet Algorithm better?
- In the normal Verlet Algorithm big numbers are subtracted from each other, which introduces rounding errors
- the Velocity-Verlet-Algorithm these calculation are seperated into different steps, so that no big errors are introduced

What are the disadvantages of the Velocity-Verlet-Algorithm?
- High computation time
- Velocities are only approximated between the time steps where the position of the particles is calculated

How does the predictor-correcor-algorithm work?
Read in a book!

The energy drift for the Velocity-Verlet-Algorithm and the predictor-corrector scheme are very low. What does this have for consequences?
No artificial cooling is necessary

What are the problems by defining stress in a DEM simulation?
- Discrete nature of material
  - So, no real continuum model

How can one solve this problem?
By using a proper averaging process

How does the stress formulation process look like?
- At first find a representative volume element (REV)
  - REV must be much smaller than the system size
- apply continuum mechanics

How is the definition of elasticity in granular matter?